Numerical Study for CFRP Strengthening of RC Columns for Blast Resistance

Saleh Alsayed*, Husain Abbas* and Yousef Al-Salloum*

* Professor,  Specialty Units for Safety and Preservation of Structures, Department of Civil Engineering, King Saud University, Riyadh 11421, Saudi Arabia

# Introduction

Structures all over the world have become recently susceptible to the threat of terrorist attacks, accidental explosions. Buildings and critical infrastructure vulnerable to explosions include government buildings, embassies, financial institutions, densely populated commercial structures, and other buildings of national heritage or landmarks. Consequently, a number of concerns have been raised on the vulnerability and behavior of these structures under extreme loadings.

The strengthening of reinforced concrete (RC) column for improving blast resistance has been studied experimentally and analytically by many investigators. Crawford et al. [1, 2] conducted experiments for studying the blast vulnerability of a square and circular column of a multi-storey building. The columns were retrofitted using CFRP wraps for shear enhancement and flexural enhancement. Riisgaard et al. [3] studied two polymer reinforced compact reinforced concrete (PCRC) columns subjected to close-in detonation. Berger et al. [4] performed blast testing on scaled reinforced concrete columns to study the behavior of different types of strengthening of Steel Reinforced Polymer (SRP), CFRP and SRP/CFRP hybrid combination. All results showed that composite retrofits could have a beneficial effect on the performance of the columns and therefore prevent progressive collapse.

The research carried out in the area is mostly qualitative and the behavior of FRP-strengthened structures under blast loading is not well understood and no proper design guidelines are available. The present study aims to analyze a RC circular column for investigating the role of CFRP in improving the collapse behavior thus avoiding the progressive collapse. The study considers different charge weights at varying stand-off distances.

Finite Element Modeling

The column selected for the study is a typical circular column of 600 mm diameter and 4 m high. The column is reinforced with 1616 longitudinal bars and 10@200 mm c/c as ties. The concrete grade of the column is taken as M30. The clear concrete cover to the ties is taken as 30 mm. Two layers of 1mm thick CFRP were thus applied as hoops for enhancement of shear strength and concrete confinement and two layers were provided along the length of the column, with fibers running in the vertical direction, to increase its flexural capacity.

LSDYNA [5], a general purpose finite element program was used to develop the 3D model of the column. Two cases were considered in the modeling of the column. The first case involved the column to be modeled without any strengthening and the second case involved strengthening of the column with Carbon Fiber Reinforced Polymer (CFRP) sheets. Damping has been ignored, as it has a negligible effect for short duration, impulsive loads. A combination of eight and six node solid elements was used to model the concrete volume. The longitudinal reinforcing bars and ties were modeled using 2-node Hughes Lui beam elements.  For the modeling of CFRP sheets, 4-node shell elements were employed. Perfect bond was assumed between rebar elements and the surrounding concrete volume and also between the FRP and the concrete substrate.  Fig. 1 details the mesh discretization for the concrete elements, the CFRP elements and the reinforcing cage used in the study. The total numbers of elements in the model are 18592.

Fig. 1. Mesh discretization of column section and rebars

The Karagozian & Case (K&C) model, designated as Material type 072R3 in LSDYNA [5], was employed to represent concrete for the column.  The model is specially designed for predicting the response of concrete under blast loads. The reinforcement was modeled using material type 024 to model the elasto-plastic response with strain rate dependency. In order to model the CFRP material, material type 054-055 was utilized, which is capable of defining orthotropic material characteristics. The laminated shell theory was used for the purpose of correcting the assumption of a uniform constant shear strain throughout the thickness of the composite shell, thus avoiding very stiff results. The concrete elements in the RC column were allowed to erode when the principle tensile strain reached 50%.

Analysis Results

Fixed boundary conditions were assigned for the top and bottom nodes of the column. The axial load acting upon the column due to dead plus live loads from upper stories was applied as nodal loads at the column top. This axial load was applied as a ramp function over a period of 0.5s.

Different charge weights of 100, 200 and 500 kg equivalent weight of TNT at stand-off distances of 1, 4 and 15 m were considered in the study. Both the un-strengthened and CFRP- strengthened columns were subjected to these blast loads. The blast loads impinging on the contact segments of the column were calculated by the software using ConWep. The contact segments of the blast were the solid elements of the front face of the column which were taken to be in contact with the blast. The vertical height of the charge was taken as 1.0 m above the base of the column because the explosive is assumed to be carried in a vehicle. Thus, the shock transmitted to the column through ground gets diminished due to which it has been ignored in the analysis. The blast loading was set to trigger at 0.5 s.

The peak lateral and permanent displacements of column for the blast scenarios considered in the analysis are given in Table 1.

Table 1: Peak and permanent lateral displacement of column*

| Charge weight (kg) | Peak lateral displacement (mm) |  |  | Permanent displacement (mm) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | d=1 m | d=4 m | d=15m | d=1m | d=4m | d=15m |
| Column without retrofitting |  |  |  |  |  |  |
| 100 | 277.5 | 10.5 | 0.9 | 260.2 | 4.0 | 0.1 |
| 200 | 489.5 | 41.1 | 1.8 | 478.9 | 20.4 | 0.1 |
| 500 | ∞ | 214.7 | 4.2 | ∞ | 173.6 | 0.5 |
| Retrofitted column |  |  |  |  |  |  |
| 100 | 61.3 | 8.9 | 0.7 | 53.7 | 2.0 | 0.1 |
| 200 | 314.9 | 16.3 | 1.4 | 294.9 | 6.4 | 0.2 |
| 500 | ∞ | 45.0 | 3.5 | ∞ | 30.6 | 0.5 |

* d = stand-off distance

The charge weights of 500 kg at a stand-off distance of 1.0 m completely destroyed both the columns with and without CFRP strengthening. So it can be assumed that the columns within the focus of a blast of this magnitude would be totally destroyed and may not be protected by retrofitting.

The retrofitting of column reduces the peak lateral displacement considerably. The retrofitting of column reduces the peak displacement by 21% when the damage to the column is almost negligible i.e. when the intensity of blast is least severe (100 kg charge weight at 15 m stand-off distance). A study of all blast cases considered indicates that the reduction of peak displacement varies from 8% for 100 kg charge weight at stand-off distance of 4 m to 79% for 500 kg charge weight at a stand-off distance of 4 m.

At 15m stand-off distance, the blast of even 500kg charge weight does not cause any significant damage to the column even without retrofitting. Considering 30mm as the acceptable permanent lateral displacement for the column, at 4m stand-off distance, blast of 100kg charge weight may be resisted by the column even without retrofitting, whereas, 200 and 500kg charge weights may be resisted by the column after retrofitting. At a stand-off distance of 1 m, the blast of even 100 kg may not be resisted by even the retrofitted column. The increase in the number of layers of CFRP may however help the column to resist it.

State of Stress and Consequent Damage

Table 2 report the results of analysis for one blast load case for column with and without CFRP strengthening. As seen from the table, it is clear that the displacement experienced by the retrofitted columns is much lower compared with the un-strengthened columns.

Table 2: Results for 100 kg charge weight at 1 m stand-off

Column without retrofitting

Concrete: Concrete was completely destroyed over the bottom 1/3 height. Severe dilation of concrete was noticed at mid-height and slight dilation was found near the top. The column rendered inadequate for service. Longitudinal reinforcement: No breakages were found in the bars. Maximum tensile stress in the bars was 591MPa. Shear reinforcement: No breakages in the ties were found. Maximum tensile stress of 497MPa was observed suggesting yielding of rebars.

Retrofitted Column

Concrete: Damage to concrete was seen at the bottom 0.5m height of the column. The FRP material protected the concrete from any severe damage. FRP material: Partial tear of the FRP material was noticed on the side facing the blast wave and on the opposite face. Longitudinal reinforcement: There was no breakage in the steel bars but many bars were bent. Maximum tensile stress of 502MPa was observed suggesting yielding. Shear reinforcement: No breakages were observed in the ties. Tensile force data suggests some of the bars might have yielded. Maximum tensile stress was 667MPa.

Conclusions

The charge weights of 200 and 500 kg at 4 m stand-off distance may be resisted by the column after retrofitting.  However, the increase in the number of layers of CFRP may help the column to resist even slightly more intense blasts. Even a light retrofitting considered in the study provided considerable resistance to blast loads, and thus contributed greatly to impeding the onset of progressive collapse for moderate blasts. The nature of the failure for CFRP-wrapped columns was also less explosive, thereby protecting loss of human life and property.

References

- Crawford, J.E., L.J. Malwar, J.W. Wesevich, J. Valancius and A.D. Raynolds (1997). "Retrofit of Reinforced Concrete Structures to Resist Blast Effects," ACI Structural Journal, 94(4): 371-377.

- Crawford, J.E., L.J. Malwar and K.B. Morrill (2001). "Reinforced Concrete Column Retrofit Methods for Seismic and Blast Protection," Proc. of Society of American Military Engineering Symposium on Compressive Force Protection, Charleston, USA.

- Riisgaard, B., A. Gupta, P. Mendis and T. Ngo (2007). "Finite Element Analysis of Polymer Reinforced CRC Columns under Close-in Detonation," Proc. of 6th European LS-DYNA User's Conference, Gothenburg, Sweden.

- Berger, J-O, P.J. Heffernan and R.G. Wight (2008). Blast Testing of CFRP and SRP Strengthened RC Columns. In: Structures under Shock and Impact X, The Built Environment volume 98. In: Jones N, Brebbia CA, editors. Transactions of the Wessex Institute, WIT Press.

- LSDYNA User's Keyword Manual, (2007). Vol. 1, Ver. 971. Livermore Software Technology Corporation.